## Slide 1
AVTC Model Based Design Curriculum Development Project

## Slide 2
An Introduction to
Modeling an
Energy Storage System (ESS)
Lesson 4.2
Short Circuit in Battery Cells
Mohammad Ghanaatpishe
Donald Docimo
Hosam Fathy

## Slide 3: Motivation to Study Electric Shorts
The field failures of lithium-ion cells due to internal short circuits are a significant concern to the electric vehicle market.[2]
The probability of their occurrence is very low, but the consequences have the potential to be catastrophic and they are not easily detected.[2]
They usually affect the cell permanently and the results range from a rapid self-discharge to explosion of the cell.

## Slide 4: Short Circuit Types
In general, electric shorts can be classified into internal or external.
  An external short occurs by touching the conducting tabs through a direct metal media.
  An internal short happens when electrons produced in the negative electrode of the cell, find a direct way through the damaged separator to get to the other electrode.

## Slide 5: Short Circuiting Reasons
Internal shorts can develop from a variety of sources including
  manufacturing defects
  physical abuse
  separator wear-out
  dissolution/deposition of electrode materials
  lithium plating
  dendrite formation[2]
It is important to note that most of these can develop over time under normal use or abuse conditions.[2]

## Slide 6: Hard Short vs. Soft Short
Internal short circuits are also classified based on the severity of their consequences.
Soft Short
  will only cause an elevated self-discharge
  self correcting is possible due to melting of the small regions in contact caused by the high current flow.
Hard Short
  Causes extremely high current flow and complete discharge resulting in permanent damage to the cell.
  The excessive temperature rises could lead to thermal runaway.

## Slide 7: Thermal Runaway
Several exothermal abuse reactions could occur within a cell, in which different components of the cell take part. Each of these reaction has its own onset temperature.[3]
The heat generated from these reactions almost doubles for every 10˚C temperature rise. But, the rate of heat dissipation increases only linearly.[1]
The heat is build up in the cell which increases internal temperature.[1]

## Slide 8: Thermal Runaway
The rise in the temperature speeds up the abuse chemical reactions.[3]
As a result, the impedance of the cell decreases which allows higher currents to flow into the cell.[1]
Higher currents generate more joule heating and further increase the cell temperature.[1]
The heat generated from the abuse reaction with the lowest onset temperature triggers the next one.[3]

## Slide 9: Thermal Runaway
These chain reactions cause an uncontrollable release of energy which could lead to the destruction of the cell. This phenomenon is called thermal runaway.
So, it is important to maintain the temperature of the cell below a limit different for different cell chemistries.
The abuse chemical reactions happening in anode usually have the lowest onset temperature and determine the operational temperature limits of a cell.[3]

## Slide 10: Variables Affecting Cell Short Circuiting
There are several variables that can affect response of a given cell to an internal short including:
  Temperature[3]
  State of the charge[3]
  Cell Capacity[3]
  Nature of the short[3]

## Slide 11: Temperature Effects
As described earlier, the onset of each abuse reaction occurs at a specific temperature.[3]
In a preheated cell, the margin for safety is reduced.
Since the temperature gradient is reduced when a short occur at higher ambient temperatures, the heat transfer is also reduced.[3]

## Slide 12: State of Charge Effects
The anode of a lithium ion cell is far more reactive when at the fully charged state.[3]
In addition, the reactions involving lithium are usually exothermic.[3]
As a result, a fully lithiated anode is several times more likely to be prone to runaway.[3]

## Slide 13: Cell Capacity
The cell capacity determines the local power due to current flow across the short-circuit.[3]
Also, the availability of reactants for the runaway reactions is more for cells with larger capacities.[3]
Hence, larger cells are more in dangerous when an electrical short occurs.

## Slide 14: Short Circuit Nature
In a lithium ion cell, four different short-circuit scenarios are probable:
  The short between the two current collectors (copper and aluminum).[3]
  The short between the copper current collector and the cathode active material.[3]
  The short between the aluminum current collector and the anode material.[3]
  The short between the active materials on both the electrodes.[3]

## Slide 15: References
[1] C. Rahn, C.Y. Wang, “Battery Systems Engineering,” Chichester: John Wiley & Sons, 2013.
[2] C. J. Orendorff, E. P. Roth, Ganesan Nagasubramanian, “Experimental triggers for internal short circuits in lithium-ion cells”, Journal of Power Sources 196, pp. 6554–6558, 2011.
[3] S. Santhanagopalan, P. Ramadass, J. Zhang, “Analysis of internal short-circuit in a lithium ion cell”, Journal of Power Sources 194, pp. 550–557, 2009.