## Slide 1
AVTC Model Based Design Curriculum Development Project

## Slide 2
An Introduction to
Modeling an
Energy Storage System (ESS)
Lesson 5.2
Battery State of Health
Donald Docimo
Mohammad Ghanaatpishe
Hosam Fathy

## Slide 3: Aging and Degradation
Over time, a battery cell ages.
  Performance decreases.
  Degradation is directly related, and is usually associated with the loss of active material or physical characteristics.
  Changes how a battery behaves dynamically.[1]
The mechanisms behind this are complex and can depend on: [1]
  Manufacturer
  Chemistry of the cell, specifically the positive electrode
This lesson analyzes LiFePO4 battery chemistry.

## Slide 4: Negative Electrode Degradation
Solid/Electrolyte Interface (SEI) layer growth: a necessary layer for conducting ions that consumes Li+, but as a result removes active material. If disconnected from electrode, resistance increases further.[2]
Lithium can be corroded, which results in a loss of active material.[1]
Lithium plating, generally caused at low temperatures or voltages, causes a loss in lithium.[1]

## Slide 5: Positive Electrode (LiFePO4) Degradation
Many of the same reasons as the negative electrode
SEI layer formation is generally much smaller than with the negative electrode [3]
  At high temperatures, this isn’t necessarily true.
Iron particles from the positive electrode can produce a interfacial film on the negative electrode [3]

## Slide 6: Important Parameters Associated with Aging
Internal resistance/impedance
  Grows larger over time through cycling of the battery
Capacity of the battery cell
  Decreases over time through cycling of the battery
  When capacity is at about 80%, the battery generally considered dead [1]

## Slide 7: Power Fade
Lower availability of power [1]
  Mainly associated with internal impedance rising[1]
Causes
  Contact losses of SEI layer [1]
Effects
  Energy is wasted through dissipated heat [1]
  Aging can be accelerated further [1]

## Slide 8: Capacity Fade
Lower amounts of energy can be stored within the battery[1]
  Related to capacity
Depends mainly on: [1]
  Porosity: Holes in the electrodes that allow the electrolyte to seep through
  Stoichiometry: loss of active lithium material through side reactions
  Both of these can be seen through the aging mechanisms reviewed earlier
Effects
  With less energy that can be stored in the battery, an HEV won’t be able to operate as efficiently.

## Slide 9: Battery State of Health (SOH)
Used to quantify aging of a cell
Most commonly defined as: [1]
Capacity is hard to find
  An effective method is to fully charge and discharge a cell using a very small current [1]
  Cannot be measured in most practical applications[1]

## Slide 10: Estimating State of Health in Hybrid Electric Vehicles
Instead of attempting to measure capacity, capacity loss can be correlated to a more measurable parameter [1]
  Most parameters do not have appropriate correlations with capacity fade
  Internal resistance rise can be associated with capacity loss [1]
Environmental effects must be accounted for [1]
Temporary performance changes need to be discounted [1]

## Slide 11: SOH Estimation Correlation
Correlation between internal impedance rise and loss of capacity:[1]

## Slide 12: References
[1] C. Rahn and C.Y. Wang. Battery Systems Engineering. Chichester: John Wiley & Sons, 2013.
[2] J.S. Newman and K.E. Thomas-Alyea. Electrochemical Systems. 3rd ed. Hoboken, NJ: J. Wiley, 2004.
[3] M. Kassem, J. Bernard, R. Revel, S. Pélissier, F. Duclaud, and C. Delacourt, “Calendar aging of a graphite/LiFePO4 cell,” Journal of Power Sources, vol. 208, pp. 296–305, Jun. 2012.