## Slide 1
AVTC Model Based Design Curriculum Development Project

## Slide 2
An Introduction to
Modeling an
Energy Storage System (ESS)
Lesson 5.3
DFMEA for Power and Capacity Fade
Donald Docimo
Mohammad Ghanaatpishe
Hosam Fathy

## Slide 3: Refresher of DFMEA
Stands for Design Failure Modes and Effects Analysis[1]
Used to make sure that reasons for potential failure have been analyzed[1]
Uses a Risk Priority Number (RPN)[1]
  Severity (S), Occurrence (O), Difficulty to Detect (D)
  Rate each category from 1-10
  RPN = S*O*D
  Prioritizes risks
Redesign to lower RPN into acceptable range

## Slide 4: DFMEA of Power and Capacity Fade
Lesson 5.2 goes over the reasons and effects of power and capacity fade.
Options for dealing with these issues:
  Prevent these effects by using parameters we can measure (voltage, current, temperature)
  Plan for methods to deal with these effects at occurrence

## Slide 5: Determining RPN
Potential Failure | Why It Happens | Severity | Occurrence | Difficulty to Detect | RPN
Capacity Fade | Porosity of electrode changing and loss of active materials | 5 | 7 | 7 | 245
Power Fade | Contact losses of SEI layer | 7 | 5 | 6 | 210
The next few slides go over the reasons for these values, and how to lower RPN

## Slide 6: Capacity Fade
Capacity fade isn’t catastrophic, but it will definitely occur for all cells
The rate of capacity fade is related to the operating range of the battery[2]
Keeping the battery in safe operating ranges allows capacity fade to grow slower
  Use data from voltage, current, and temperature measurements

## Slide 7: Capacity Fade Mitigation
Monitor and limit voltage, current, and temperature of the cell
  If none of these are in extreme limits for a battery cell, then degradation effects are limited
  If limits are hit, the battery pack could be shut down to avoid severe capacity fade
Cell balancing
  Keeping all the cells at the same voltage means they should age similar, and keep the pack consistent
  See Lesson 3 for cell balancing methods
Both methods decrease occurrence and severity, and increase the ability to detect capacity fade indirectly
Make V1 = V2 = V3

## Slide 8: Power Fade
Power fade could create dangerous situations involving regenerative braking if not handled properly
  Increased internal impedance means the battery won’t be able to handle as much power.
  Braking requires large amounts of power.
  Mechanical braking is used to supplement regenerative braking by dissipating energy.
  The more mechanical braking is used because of power fade, the less efficient the HEV is.
    At high power fade, there will be no regenerative braking, and the battery loses one of it’s more important purposes in the HEV.
With data from the vehicle, the best option is not just to try to prevent it, but to deal with it when it occurs

## Slide 9: Power Fade Mitigation
Power fade produces voltage increases
  Monitoring voltage for these can indicate power fade
  Increases ability to detect power fade
If a voltage spike is observed:
  Have control scheme allow an increase in mechanical braking to dissipate energy the battery cannot handle
  Send a signal to the dashboard, indicating the battery should be checked
  These reduce the severity of power fade’s effect
Next case study looks into the effects of power fade

## Slide 10: Reevaluating RPN
RPN for all cases has been lowered to acceptable values!
Potential Failure | Why It Happens | Severity | Occurrence | Difficulty to Detect | RPN
Capacity Fade | Porosity of electrode changing and loss of active materials | 4 | 2 | 2 | 16
Power Fade | Contact losses of SEI layer | 2 | 5 | 2 | 20

## Slide 11: References
[1] Raytheon Six Sigma. (2007). Design Failure Modes and Effects Analysis (edition) [online]. Available: http://www.raytheon.com
[2] C. Rahn and C.Y. Wang. Battery Systems Engineering. Chichester: John Wiley & Sons, 2013.